## Slide 1
Argo SPAD sensor analysis
고객가치
새로운 시도
집요한 실행

## Slide 2: Argo SPAD sensor analysis
Absorption
Grading
Charge
Multiplication
InGaAs layer, Eg = 0.75eV, cutoff wavelength = 1670nm
To avoid carrier accumulation in the heterojunction interface
To provide high electric field in the multiplication region
To provide desired avalanche probability
1. InGaAs/InP SPAD system
Because of the high bandgap of InP (Eg = 1.35ev), the photons pass through the InP region.
h+
e-
InP
InGaAs
h+
e-
InGaAsP
InGaAs
InP
Photon absorption process
Photon absorption
Electron hole generation
The photons are absorbed at the InGaAs region (Eg = 0.75eV) and electron hole pairs are generated.
Hole propagation
The grading region prevents the hole from trapping at the interface between InGaAs region and InP region.
Impact ionization
The impact ionization is generated at the multiplication region.

## Slide 3: Argo SPAD sensor analysis
Overview
6. i-InGaAs / InP Interface
1. Passivation
3. Anode Contact
2. Anode Metal
4. i-InGaAs absorber
5. InP/InGaAsP Grading
SiNx : 161.4nm
InGaAsP : 46.9nm
i-InGaAs
InP buffer
InP
i-InGaAs
InGaAsP : 45.9nm
InGaAsP : 43.2nm
Ga,As↑ / In,P↓
InP
Au : 181.2nm
Ti+InP(Diffused) : 27.3nm
Au : 1.36µm
Pt : 40nm
Pt : 44.2nm
SiNx : 91.5nm
Au
Ti : 29nm
SiNx : 95.2nm
SiNx : 249.7nm
Oxygen
@Interface
i-InGaAs : 1.3µm
i-InGaAs : 1.3µm
Grading : ~136nm
InP : 4.3µm
Ti : 28.4nm
Pt : 40nm
Ti : 27.3nm
1
2
3
4
5
6

## Slide 4: Argo SPAD sensor analysis
2. Characteristics of SPAD
Material characteristics
Breakdown voltage
Quenching characteristics
Dead time
Efficiency characteristics
Photon detection efficiency
Dark count rate
After pulse
Cross talk
Timing jitter
Noise characteristics
Done in RX test
Basic setup for characterize SPAD characteristics
Attenuator attenuating the laser power down to the single-photon level.
Quenching electronics gating the SPAD
Signal generator outputs original gates and synchronized signals with the same frequency to drive a laser diode
Counter counting the triggered signal
Advances in InGaAs/InP single-photon detector systems for quantum communication

## Slide 5: Argo SPAD sensor analysis
2. Characteristics of SPAD
Photon detection efficiency
The ratio btw the number of incoming photons and the number of output current pulses
Measurement of photon detection efficiency
Starting from single pixel illumination
The target pixel starts avalanche event
Counting the avalanche event during the measurement time.
Calculating PDE based on counted photons and incoming photons
Dark count rate
The thermally generated carriers can trigger the avalanche
Even when the device is kept in dark conditions, there can be avalanche process (dark count)
Measurement of dark count rate
Protect the light propagating through the pixel
Counting the avalanche event during the measurement time
Calculating PDE based on counted signals with in the time
Test | Description | Acceptance Criteria
Array turn on voltage (V50) | Find voltage at which 50% of pixels fire | 85V ± 10V
VBR gradient | Find difference between voltage at which 85% and 15% of pixels fire at all | ≤1V
VPDE20 | Find voltage where average PDE of array is 20% | VPDE20 exists and VPDE20 ≤ V50+4.2
DCR(VPDE20) | Find exp[mean(ln)] DCR for array at VPDE20 | exp[mean(ln)] DCR for array at VPDE20 ≤ 500kHz
Breakdown voltage
The voltage at which SPAD fire
Operating region
Breakdown voltage
Inspection criteria of Argo FPA module

## Slide 6: Argo SPAD sensor analysis
2. Characteristics of SPAD
After pulse
The probability to have another count in the same pixel, that is correlated to the former one
Due to the trapping of free carriers during the avalanche
Larger the SPAD hold off time is, the smaller the after pulse probability is
SPAD gating speed
After pulse
Trade off
Dead time ↓
Dead time↑
Trapping site
Measurement of after pulse
Measure the dark count rate for specific dead time
Repeat the dark count measurements with different dead times set for the active quenching circuit
Measure the photon count rate for same dead times
Using the below equation, calculate detrap time and average after pulse
Afterpulsing Effects in Free-Running InGaAsP Single-Photon Avalanche Diodes
: dark count : photon count : after pulse count : hold-off time : detrap time
↓ Count rate per photon flux

## Slide 7: Argo SPAD sensor analysis
2. Characteristics of SPAD
Crosstalk
The hot carriers lead to intense emission of secondary photons
Some of which escape from the chip
If re-absorption takes place within the active area of a neighboring pixel, an avalanche process is triggered.
1
1
5.68µm
Can be prevented using isolation between pixel
Measurement of crosstalk
Starting from single pixel illumination
The target pixel starts avalanche event
Scanning the data for a trigger pixel that experienced an avalanche event
Search for all pixels that may have fired at nearly the same time as the trigger pixel
Analyze the temporal correlation of assumed crosstalk counts with test trigger pixel
Assumption: Any avalanche event within some ns of the trigger pixel is correlated
InP-based Geiger-mode avalanche photodiode arrays for three-dimensional imaging at 1.06um

## Slide 8: Argo SPAD sensor analysis
2. Characteristics of SPAD
Timing jitter
The total time uncertainty between incident photons and corresponding electrical signal outputs
Measurement of timing jitter
Jitter
Sending laser pulses directly to the detector
Collecting the histogram of the distribution of the delay